## Slide 1: Lightweight assistive technology: A wearable, optical-fiber gesture recognition system
Sanjay Seshan

## Slide 2: Motivation

## Slide 3: Basic idea
Transverse carpal ligament area
  Deflection occurs when fingers [tendons] are moved
How to measure deflection?
  Light

## Slide 4: Basic setup for an optic fiber
Fiber/light medium
LED
Photoresistor/LDR
LED
Photoresistor/LDR
In order to detect the deflection using a LDR, a significant amount of light must be lost when the fiber is bent

## Slide 5: Materials/Mediums proposed
Standard optical fiber
Vytaflex – a semi-transparent urethane rubber
Ecoflex – an opaque silicone
Humimic gel – a transparent synthetic gelatin

## Slide 6: LED Color
The optimal wavelength of the LDR must be determined
This does not depend on the material used
Humimic was used as a constant baseline
A 3d printed cast was used to eliminate external light
A constant depression was used to determine minimum intensity
Colour | Medium | Minimum Intensity | Maximum Intensity | delta Intensity | Notes
Large blue | Humimic #2 | 160 | 993 | 833 | 
Large red | Humimic #2 | 183 | 1013 | 830 | 
Large white | Humimic #2 | 205 | 1021 | 816 | 
Small red | Humimic #2 | 180 | 977 | 797 | 
Large red | Earth's atmosphere | 235 | 996 | 761 | Value seems to fall slowly
Large yellow | Humimic #2 | 210 | 971 | 761 | 
Small green | Humimic #2 | 189 | 937 | 748 | 
Large blue | Earth's atmosphere | 228 | 957 | 729 | 
Large green | Humimic #2 | 185 | 850 | 665 | Value seems to fall rapidly
Small red | Earth's atmosphere | 245 | 864 | 619 | Value seems to fall slowly
Small green | Earth's atmosphere | 253 | 775 | 522 | 
Large green | Earth's atmosphere | 240 | 720 | 480 | Value seems to fall rapidly

## Slide 7: Problems with each material
Optic fibers were too perfect and there was no light deflection, even when bent over 90 degrees.
  The internal reflection is too high
  A non-ideal optical fiber is needed so that light is lost when bent
Ecoflex was too opaque and did not permit any light from the LED to pass
Humimic was too soft and melted/tore due to the body heat.
  Humimic melts at about 50 degrees; body heat is about 40

## Slide 8: Gestures tested
Extend
Fist
One
Two

## Slide 9: Collecting data
1 Arduino Uno
XXX Arduino wiring diagram here

## Slide 10: Sample data
Uses exponentially weighted moving averages
XXX
Chart: Basic comparison of light deflections over time when extending the hand in cycles